|  |  |  |  |
| --- | --- | --- | --- |
|  | | |  |
| **Annexure MRTS101.1 (November 2022)** | | |
| **Aggregates for Asphalt** | | |
|  | | |
| **Specific Contract Requirements** | | |
|  | | |
| **Contract Number** | |  |
|  | | | |
| Note: | Clause references within brackets in this Annexure refer to Clauses in the parent Technical Specification MRTS101 unless otherwise noted. | | |
| |  |  |  | | --- | --- | --- | | PAFV requirement for surfacing course (Table 7.1) | | | | **Project Specific Requirement** | **Minimum Requirement** | | Polished Aggregate Friction Value (PAFV) (for use in surfacing course) |  | | If no indication is given, the minimum PAFV for the aggregate used in the surfacing course shall be 48. | |  |  | | --- | | The following PAFV requirements are typically adopted for Transport and Main Roads projects (other than for high crash risk and/or high skid demand sites) for asphalt surfacing layers:   * minimum 48 where the 20 year design traffic volume is ≥ 1 x 107 Equivalent Standard Axles (ESAs) and * minimum 45 where the 20 year design traffic volume is < 1 x 107 Equivalent Standard Axles (ESAs).   For high crash risk and/or high skid demand sites, a higher minimum PAFV may be specified. | | | | |